Instructions for limestone, travertine,

cement based terrazzo and concrete.

These instructions would apply equally to limestone, travertine, cement based terrazzo and concrete. Ignore all the instructions for staining unless you are planning on staining concrete that is the only difference. 

If the surface is rough or damaged severely enough that very low grit metal
bond diamonds must be used then just make sure your last metal bond diamond
is 100 grit. After that the whole restoration can be performed with the
Cheetah Pads.

If the surface is smooth and the damage is not severe you may be
able to Start with Step-1 (damage can be seen and felt with fingers and/or
fingernail) or even Step-2(you can see surface etching or traffic wear
damage but can't really feel it) 

Start with Cheetah Pads or Pucks Step-1 by testing a small section 5ft by 5ft. Work
the area (ALWAYS USE CHEETAHS WET-NEVER ALLOW THEM TO RUN DRY) for 30 seconds total. 

Squeegee a small area, wipe clean, and dry with fan or heat gun or hair drier. 

Look closely to see if 100% of the scratch pattern from the metal bond
diamond cut has been fully removed. Even though Step-1 cuts very rapidly and
creates a very thick slurry you'll know you're done because the surface
should be very smooth and there should be no visible scratch pattern. If 30
seconds isn't enough, repeat as many times as needed in 30 second increments
until you determine exactly how much time a 5x5 area takes to complete that
particular step cheetah puck. 

---USE A LARGE DIGITAL DISPLAY COOKING TIMER TO ACCURATELY TRACK TIMES---

Once your time per 5x5 area is determined, divide the time it took by 25 and
you now know how many square feet you can complete in how much time. Just
repeat that exact amount of time or more (never less time) on the whole area
working at the sq ft rate you determined.

Rinse thoroughly and vacuum well as you go but pull the bulk of the slurry
with you keeping it under the cheetahs to accelerate cutting.  After rinsing
and vacuuming run a wet micro fiber flat mop over the area to ensure you've
removed 100% of any abrasives left behind after each step. Use a clean micro
fiber each time. 

Now repeat the same test procedure but with Step-2 Cheetah Pads or Pucks. You'll do
this once on each step to determine best results and optimum efficiency. 

Staining or dying should be done after step 2 once the surface is completely
clean and dry. Apply two to four coats acetone stain (AmeriPolish Acetone
Concrete Stain) according to manufacturer instructions. Then liberally apply
our Lithium Silicate Hardener and move it around keeping the surface wet for 15-20 minutes then allow to absorb until it is dry to the touch. Repeat Hardener application
1-3 times until it seems to stop absorbing quickly. 

LET IT CURE OVER NIGHT – DO NOT USE FANS

Now you're ready for Step-3 test. Determine your cut rate and do the whole
area just as you did on previous steps. The longer you run steps 3&4 the
higher gloss you'll achieve. An easy way to know you gotten the maximum
result from each step is as follows. 

Once you think you've completed a 5x5 section, go over 1/2 of the section
for another 30 seconds. Vacuum and dry the area. Looking straight down at
the reflection of a light source on the ceiling move from one side to the
other. Do both areas look identical? If yes, that amount of time is perfect.
If the reflection is crisper and brighter in the 1/2 you spent an extra 30
seconds on then you need to work the area another 30 seconds or more. Retest
in increments of 30 seconds. 

You'll repeat this process on step-4 and then stain the surface again to
deepen the color. Apply another lighter coat of our Hardener and allow it to
dry at least two hours preferably over night. 

Now you're ready to start polishing.

After finishing step 4

Wet polish with 8,000 or 11,000 grit monkey pad

Dry the surface

Apply last coat of stain according to stain manufacturer specs

Clean up excess stain according to stain manufacturer specs

Mix nano guard 1 gal nano: 4 gal water

Apply very light but uniform coat with clean micro fiber flat mop as
quickly as possible to avoid streaks (apply one small manageable area before
applying to next area) similar to top coating wood floor. 

Allow 30 min dry time after each coat. Do not use fans! It’s important to let it dry thoroughly on its own to allow the chemical reaction to happen.

Dry buff off ALL excess nano on surface. Should only take a few seconds per
sq ft. Only enough to polish away streaks and any nano on surface. We do not
want a topical coating. It’s meant to only fill pores not top coat. 

Repeat application of nano guard 2-4 times (use your best judgment)

DRY BUFF AFTER EVERY APPLICATION OF NANO GUARD

I prefer a high speed burnisher but a 175 or 300 rpm floor buffer will do as
well.